## Slide 1: Evaluation of two degradable mulches in sweet pepper greenhouse cultivation
Piotr Siwek, Andrzej Kalisz, Iwona Domagała-Świątkiewicz
Michał Puchalski and Konrad Sulak

## Slide 2: THE AIM OF RESEARCH in BIOGRATEX
Formulation of degradable nonwovens for
soil mulching and direct covering of plants
Assessment of vegetables yield quantity and quality
Assessment of nonwovens durability in field conditions
Assessment of biodegradable pots for the transplants
Assessment of strings for plants fixing in greenhouses
Assesment of degradation progress in the field

## Slide 3
Spun-bonded technology
A scheme of the spun-bonded line. (1)-air attenuator, (2) – belt, (3) compaction roll, (4) heated calender
In spun-bond technology manufacture of fibre and non-woven production are combined in one process. The essence of this technology is to obtain in a short process of manufacturing, flat textile product with characteristics similar to technical fabrics at a much lower price. Due to the high efficiency and high speed of non-woven manufacture, this technology is preferred for economic reasons. Environmental benefits resulting from the use of spun-bonded technology is the lack of side products, both solid and gas and a small amount of waste.
Selection and characterization of additives (e.g
photodegradation activator)
Pre-mixing of polymer and additives
Production of non-woven using a mixture of base polymer and modifying the concentrate.
Pre-mixing of polymer and nano-additives . Developing optimal form of modifying the concentrate.
The steps of the preparation of modifying non-woven for agriculture
The non-woven fabrics were formed at the Institute of Biopolymers and Chemical Fibres in Łódź. The process parameters were as follows: a temperature in the range from 215°C to 225°C and a polymer throughput in the range of 0.34-0.43 g/min/hole can be used. The calender temperature was varied from 95 to 125°C.
Microphotos of PP nonwoven

## Slide 4: Direct covering with nonwovens of the winter leeks
20.11.2011

## Slide 5: Plants of the leeks after the winter 2011/2012
4.04.2012

## Slide 6: Leeks grown without and with the nonwoven, April 2012
18.04.2012 r.

## Slide 7: Yield of the winter leeks under direct nonwoven covers, kg m-2
POIG.01.03.01-00-007/08
Kind of cover | Market. yield kg m-2 |  | Dry matter % |  | Total sugars % | 
 | 2012 | 2013 | 2012 | 2013 | 2012 | 2013
PLA 50 g m-2 | 2,00 b | 2,20 b | 21,2 b | 21,5 a | 4,07 b | 4,69 c
PP ph. 50 g m-2 | 2,15 b | 2,04 b | 13,9 a | 24,9 b | 3,35 a | 3,97 b
PP 50 g m-2 | 1,75 b | 2,06 b | 17,1 b | 23,4 b | 4,82 b | 3,41 b
Control | 1,02 a | 1,40 a | 18,0 b | 22,0 a | 3,90 a | 3,01 a

## Slide 8: Mulching with nonwovens of the soil in cucumber cultivation

## Slide 9: Materials and methods of experiment
The experiment with degradable soil mulches in sweet pepper cultivation was carried out in 2012 and 2013 in plastic greenhouse FARMER 4,6 x 9 x 30 m covered with double Gemme 200 mic. film.

## Slide 10: Kind of mulches
Three kinds of degradable materials were used:
- polyprophylene non-degradable (PP Agro)
- degradable PP with 0,02% photoactivator (PP ph.)
- polylactide (PLA)
Control treatment was the plots without mulching.
The non-woven fabrics all with the surface mass 50 g m-2
were formed by a spun-bond technique on a laboratory line, designed and constructed by the Research and Development Centre of Textile Machinery Polmatex-Cenaro, Poland.

## Slide 11: Plant cultivation
Seeds of the ‘Collado’ F1 cultivar (blocky type, Fito Semilas) were sown on 20 February. The transplants were planted on 4 May 2012 and 10 May 2013 in each hole in the mulch, with row and plant spacing of 80 × 60 × 50 cm in four replications of 20 plants each
The two-shoot plants were pruned regularly, as at the every node was leaved only one fruit. Yielding started: 29 June 2011 and 12 July 2012 and ended 29 September and 9 October respectively.

## Slide 12: Strings for plants fixing
PLA (polylactide)

## Slide 14
Mulch type | I grade |  | II grade |  | Marketable yield | 
 | fruits per 1 m2 | kg m-2 | fruits per 1 m2 | sz. m-2 | fruits per 1 m2 | kg m-2
PP 50 photo. | 23 a | 4.12 a | 0.6 a | 0.36 a | 23.6 a | 4.48 a
PLA 50 | 24 a | 4.17 a | 0.6 a | 0.32 a | 24.6 a | 4.49 a
PP 50 | 25 a | 4.51 a | 0.6 a | 0.29 a | 25.6 a | 4.80 a
Control | 21 a | 3.61 a | 0.2 a | 0.32 a | 21.2 a | 3.93 a
Yield of sweet pepper cultivated on different mulches in a plastic greenhouse in 2012 and 2013
Mulch type | I grade |  | II grade |  | Marketable yield | 
 | fruits per 1 m2 | kg m-2 | fruits per 1 m2 | kg m-2 | fruits per 1 m2 | kg m-2
PP 50 photo. | 29 a | 4.67 a | 1.0 a | 0.12 a | 30.0 a | 4.79 a
PLA 50 | 36 b | 5.47 ab | 2.1 a | 0.18 a | 38.1 b | 5.65 ab
PP 50 | 36 b | 5.68 b | 1.2 a | 0.19 a | 37.2 b | 5.87 b
Control | 39 b | 6.12 b | 1.3 a | 0.18 a | 40.3 b | 6.30 b

## Slide 15
Mulch type | L-ascorbic acid (mg 100 g-1 FW) |  | Dry weight (% FW) |  | Soluble sugars (% FW) | 
 | 2012 | 2013 | 2012 | 2013 | 2012 | 2013
PP 50 photo. | 84.8 b | 67.6 a | 5.81 a | 5.86 a | 2.47 a | 2.18 a
PLA 50 | 73.0 a | 78.4 a | 5.78 a | 5.78 a | 2.24 a | 2.34 a
PP 50 | 72.1 a | 104.5 b | 5.90 a | 5.97 a | 2.90 a | 2.49 a
Control | 81.6 b | 108.5 b | 5.80 a | 6.10 a | 2.33 a | 2.45 a
Chemical constituents of sweet pepper cultivated on different mulches in a greenhouse, 2012-2013.

## Slide 16
CONCLUSIONS
The influence of degradable and non-degradable mulches on the soil
temperature was negligible in comparison with non-mulched plots
Microclimatic factors were similar in whole area of the greenhouse
The yield of pepper did not differ significantly between the treatments
The dry weight and soluble sugars of the plants were also similar
After first season of tests, the supramolecular changes of polymers
suggest the degradation only polypropylene with iron stearate but these
changes did not excluded use of this material in the second season
The supramolecular structure of polypropylene changed insignificantly,
this confirmed the resistance of this material to degradation factors

## Slide 17
This work was partially financed by European Regional Development Fund in the frame of “Biodegradable fibrous products”
Project (acronym BIOGRATEX) No. POIG 01.03.01-00-07/08-09
and from funds of statuary activity by Lodz University of Technology
Part of work was financed from funds of Ministry of Science and Higher
Education of Republic of Poland.
ACKNOWLEDGEMENTS
Thank You for the attension