## Slide 1: Effect of greenhouse films on climate, energy, light distribution and crop performance-measuring film properties and modeling results
S. Hemming, E. Baeza Wageningen University & Research,
Business Unit Greenhouse Horticulture
esteban.baezaromero@wur.nl ; silke.hemming@wur.nl
XXIst CIPA Congress, Bordeaux-Arcachon, France,

## Slide 2: Protected cultivation = modification of the aerial growth factors
Field cultivation = improvement of root-zone environment
Protected cultivation = improvement also of the aerial environment
The properties of the shelter determine the aerial factors inside

## Slide 3: Limiting factor concept
[H2O]
temperature
radiation
H2O
Ambient
Root zone
Minerals
[CO2]
Water, minerals, carbohidrates
€
A sub-optimal factor can not be compensated optimizing the others

## Slide 4
Plants need: Light
temperature
Plants give:
Vapour
humidity
Plants need:
Water & nutrients
Plants need:
CO2
CO2
Cecilia Stanghellini
Important function greenhouse film
Photosynthesis, growth, development, production
tPAR, tNIR
tIR, e
ac

## Slide 5: How do greenhouses work?
photosynthesis + heat
UV PAR NIR
Morphogenesys
Color & Insects
temperature inside
Solar energy is trapped  heat
Excess energy is “ventilated away”
heat
Drawbacks of ventilation:
impossible to control [CO2]
way-in for pathogens
way-out for predators
[spectral] reflectivity & transmissivity
diffusivity
Ventilation capacity

## Slide 6: Night-time
temperature
apparent sky temperature
Ambient temperature
heating
TIR emissivity/ transmissivity
Heat conductance

## Slide 7: Heat IR loss from greenhouse Transmission t, reflection r, absorption a
Transmission tIR
Thermal infrared
IR
Reflection rIR
Absorption aIR
tIR+rIR+e=1
=Emission e

## Slide 8: The desired spectral properties of covers…
“visible” light (PAR)
Near Infrared (NIR)
Thermal infrared (TIR)
τ as high as possible
ρ high to cool
ρ low to keep warm
τ ; ε low to keep warm
τ ; ε high to cool
...change with external conditions: location and time

## Slide 9: The adaptive greenhouse...
Greenhouse model
Crop model
Control
activo
Climate
Greenhouse structure
Ventilation capacity
Ventilation management
Optical properties cover
Insulation (including screens)
Temperature
Humidity
Solar radiation
Wind
Heating
CO2
Cooling
Artificial light, etc
Required resources
Better possible passive greenhouse
Productivity
fuel
electricity
CO2
water
©Wageningen Research

## Slide 10
Greenhouse climate and energy model

## Slide 11
Crop growth model

## Slide 12
Greenhouse climate model
Economic model
Crop growth model
Taiwan

## Slide 13: Microclimate prediction under different plastic films in the tropics
Taiwan
Notes: Different regions in the world

## Slide 15
Advise: to use a plastic film that is diffuse/high transmission, also to thermal radiation (to help reduce extreme greenhouse temperatures)

## Slide 16: Energy consumption prediction under different coverings in a humid subtropical climate
Japan
Notes: Different regions in the world

## Slide 17
Radiometric properties of different greenhouse covering materials

## Slide 18
Advise: economic model showed that single ETFE was better option, despite of lower energy use efficiency

## Slide 19: Greenhouse crop production under different coverings in a cold winter climate
Notes: Different regions in the world

## Slide 20
Standard glass (hemispherical light transmission of 81,9%) vs glass with a new coating (hemispherical light transmission of 85,6%)
 | Tomato(+%) | Sweet pepper(+%) | Cucumber(+%)
Light in greenhouse | 4,5 | 4,5 | 4,5
Photosynthesis | 3,2 | 3,0 | 3,1
Leaf area | 0.9 | 0,2 | 0,0
Plant weight | 3,1 | 1,6 | 2,2
Yield | 3,2 | 2,9 | 5,2
 | Chrysanthemum (+%) | Gerbera(+%) | Rose(+%)
Light in greenhouse | 3,8 | 3,6 | 2,4
Photosynthesis | 3,2 | 2,6 | 1,5
Leaf area | 3,0 | 0,0 | 1,3
Plant weight | 3,0 | 2,6 | 1,2
Yield | 3,4 | 2,6 | 2,8
Crop growth parameters, all values (in %) show the beneficial effect of a glass with higher light transmission

## Slide 21
Conclusions
Greenhouse models are suitable to compare different covering materials with each other while keeping all other factors constant
This gives fast answers without very intensive and costly agronomic trials.
Models shown in this paper have been intensively validated with experimental data in different climate conditions, for different greenhouse types and different crops and cropping strategies.
The described models always assume a “good grower”. More conservative yield values can be obtained by using correction.
Connecting model output with economic figures makes it possible to define interesting business cases for growers
Help growers in their decision for a suitable covering or can help producers to develop new materials for the greenhouse market.

## Slide 22: Wageningen University & Research, BU Greenhouse Horticulture
Innovations for the horticultural sector
THANKS A LOT FOR YOUR ATTENTION!