## Slide 1: Use of photo-catalysis in greenhouse film application and its experimentation in field trials
Ermanno Traietta - Maurizio Lanza

## Slide 2: Table of Contents
Ultrabatch at glance
Greenhouse film market
Katalite Revolution
Katalite Trials in Sicily
Take Aways

## Slide 3: Table of Contents
Ultrabatch at glance
Greenhouse film market
Katalite Revolution
Katalite Trials in Sicily
Take Aways

## Slide 4: ULTRABATCH at glance
Our Mission:
“We search solution to Add Value”
Our Values:
“Partnership”
“Knowledge”
“Flexibility”
“Innovation”

## Slide 5: ULTRABATCH at glance
Polyolefin Additive Producer
20 M€ Turnover
5000 Mt/year capacity
Cutting-edge technology
Core Business: Agri-Applications

## Slide 6: Table of Contents
Ultrabatch at glance
Greenhouse film market
Katalite Revolution
Katalite Trials in Sicily
Take aways

## Slide 7: Greenhouse film market
Greenhouse effect
Antifog Effect
Service Life
Ligth Transmission

## Slide 8: Table of Contents
Ultrabatch at glance
Greenhouse film market
Katalite Revolution
Katalite Trials in Sicily
Take aways

## Slide 9: Katalite Revolution
STRENGHT
Permanent effect
Healthier crops
VALUE
+ Profits
Smart Film
IDEA
Anticipated harvest
Cost Savings
Step forward service life belief
Secure Agri-Film business

## Slide 10: Table of Contents
Ultrabatch at glance
Greenhouse film market
Katalite Revolution
Katalite Trials in Sicily
Take Aways

## Slide 11: Katalite trials in Sicily
Location: Messina
Irradiation: 150 KLy (average)
Greenhouse dimension: 8x12 m
Crop: Tomatoes (Lycopersicon esculentum) 4 plants/m2
Growth Substrate: Loam Soil
Film Data:
  Thickness: 200 µm
  Polymer: Blend of EVA/PE
  3 Layers
  Light stabilization: Cyasorb THT 6460 (1,2%)

## Slide 12: Katalite Trials In Sicily: Light Diffusion
Reference Film
Katalite Film

## Slide 13: Katalite Trials In Sicily: Antimicrobial Effect
Reference Film
Katalite Film

## Slide 14: Katalite Trials In Sicily: Antifog Effect
Reference Film
Katalite Film

## Slide 15: Katalite Trials In Sicily: Results
Reference | Year | Date of Transplant | Number of Cluster | Infected Plants (%) | Average Temperature (°C) | Average Humidity (%) | PAR (M/m2/d)
Control | 2015 | 06-Feb | 6 | 20 | 22,4 | 63 | 2431
Katalite | 2015 | 06-Feb | 9 | 5 | 21,7 | 64 | 2555
Control | 2016 | 04-Mar | 6 | 10 | 23,7 | 61 | 2489
Katalite | 2016 | 04-Mar | 8 | 3 | 23,1 | 63 | 2664
Control | 2017 | 15-Feb | 7 | 30 | 24,3 | 65 | 2461
Katalite | 2017 | 15-Feb | 9 | 11 | 23,5 | 67 | 2609
Table 1: Data were taken 90 days after transplantation date. PAR refers to the accumulated value in 90 days. Instrument errors are +/- 0,5 (°) for temperature, +/- 3 (%) for relative humidity and +/- 5 (%) for PAR readings.

## Slide 16: Katalite Trials In Sicily: Results
Reference | Year | Harvest beginning Date | Harvest End Date | Anticipation (days) | Tomatoes Clusters | Infected plants (%) | Plants Yield (Kg.) | Yield Increment (%)
Control | 2015 | 24-May | 26-Jul | - | 9 | 50 | 4,8 | -
Katalite | 2015 | 08-May | 24-Jun | 16 | 10 | 7 | 6,4 | 33,3
Control | 2016 | 08-Jun | 01-Aug | - | 8 | 33 | 4,4 | -
Katalite | 2016 | 22-May | 21-Jul | 12 | 11 | 5 | 7,0 | 59,1
Control | 2017 | 30-May | 29-Jul | - | 8 | 61 | 3,6 | -
Katalite | 2017 | 12-May | 20-Jul | 18 | 11 | 21 | 5,3 | 47,2
Table 2: Main harvest results for all three years of trials.

## Slide 17: Table of Contents
Ultrabatch at glance
Greenhouse film market
Katalite Revolution
Katalite Trials in Sicily
Take Aways

## Slide 18: Take Aways
Light Diffusion
+ Flowers
+ Clusters
Antimicrobial
Effect
- Diseases
Antifog
Effect
Hydrophilicity
Permanent
- Waste
KATALITE

## Slide 19: Take Aways
Antifog
Effect
Light Diffusion
Healthier
Enviroment
Antimicrobial Effect
Higher Crop Yield
Cost
Savings
Higher Benefits

## Slide 20: KATALITE Created for the future, available Today
Ermanno Traietta - Maurizio Lanza
Email: ermanno.traietta@ultrabatch.it